## Slide 1
Computational Materials Theory and Methods
Alexey V. Akimov
University at Buffalo, SUNY
Lecture 2:
Classical Molecular Mechanics

## Slide 2
Time and size scales for different methods of dynamics

## Slide 3
Accuracy and methodology

## Slide 4
Potential energy surface (PES)
Stationary Schrodinger Equation
Computationally expensive!
Can we fit the curves with a simple analytical function?
Within the Born-Oppenheimer Approximation

## Slide 5
Force fields (Molecular Mechanics)
Force field
functional
parameters
Numerically efficient
Has suitable derivatives
Is continuous
Physically meaningfull
Based on atom and interaction types
Minimal amount is desirable
Transferable or system-specific
Reproduce ab initio or experiment
(thermodynamic properties, spectra,
chemical reactivity, etc.)
describes covalent bonding
non-covalent interactions

## Slide 6
Bonded interactions
In quantum mechanics: bonds are everywhere “bond order”
In molecular mechanics: bonded atoms must be specified by the user

## Slide 7
Non-bonded interactions
Charges are usually constant,
but there are geometry-dependent
charge schemes (e.g. qEQ)
Accounts for the polarizability
In periodic systems, the lattice
summation methods are used,
such as Ewald sum method.
Rappe, A. K.; Goddard, W. A.
J. Phys. Chem. 1991, 95, 3358–3363.
Ogawa, T.; Kurita, N.; Sekino, H.; Kitao, O.;
Tanaka, S.
Chem. Phys. Lett. 2004, 397, 382–387.
Karasawa, N.; Goddard III, W. A.
J. Phys. Chem. 1989, 93, 7320–7327.
Chen, J.; Martinez, T. J. Chem. Phys. Lett. 2007, 438, 315–320.

## Slide 8
Atom types
Rappe, A. K.; Casewit, C. J.; Colwell, K. S.; Goddard III, W. A.; Skiff, W. M.
J. Am. Chem. Soc. 1992, 114, 10024–10035.
Wang, J.; Wolf, R. M.; Caldwell, J. W.; Kollman, P. A.; Case, D. A. J. Comput. Chem. 2004, 25, 1157–1174.
Generalized Amber FF
Universal FF (UFF)
Halgren, T. A. J. Comput. Chem. 1996, 17, 490–519.
MERCK FF 94
General purpose FFs
Specialized FFs

## Slide 9
Parameterization: Specialized FFs
MERCK FF 94
Accurate
Focus on organic molecules
Many parameters!
Halgren, T. A. J. Comput. Chem. 1996, 17, 490–519.

## Slide 10
Rappe, A. K.; Casewit, C. J.; Colwell, K. S.; Goddard III, W. A.; Skiff, W. M.
J. Am. Chem. Soc. 1992, 114, 10024–10035.
Universal FF (UFF)
Parameterization: General-purpose FFs
Not so accurate!
General purpose (e.g. organometallic)
Way fewer parameters!

## Slide 11
Polarization: Charge equilibration method
Rappe, A. K.; Goddard, W. A. J. Phys. Chem. 1991, 95, 3358–3363.
electronegativity
self-Coloumb (idempotential)

## Slide 12
Handling vdW interactions with PBC
Simulation cell vectors
Atomic coordinates
All combinations of integers
That is an infinite number of cells!
Exclude self-interactions
Dealing with the infinite number of terms
Van der Walls interactions
are short-ranged
Disregard all the interactions
for the particles separated
more than by

## Slide 13
Simulation cell
Periodic Image
Same atom/molecule
1
2
3
1’
2’
3’
3’’
2’’
Handling non-bonded interactions with PBC
If simulation cell size is larger than , it is sufficient to have only one shell of periodic images

## Slide 14
Electrostatic interactions
are long-ranged
Can not use the cutoff technique
Direct summation is slowly converging
Handling electrostatic interactions with PBC
Converges fast
in real space
Converges fast
in reciprocal space

## Slide 15
Continuity of forces
Truncation of the potential makes it
discontinuous at .
Solution: shift by the corresponding energy
shifted potential
But the forces are still discontinuous!
Solution: Modify the potential such that
the force is also continuous at shifted-force potential
potential
force

## Slide 16
Class I FFs: (diagonal terms): e.g. all bonds, all angles, etc.
Class II FFs: (+ cross-terms): e.g. add bond-angle interactions (e.g. like in MMFF94)
Classification of the FFs
Bond-order (“reactive”) FFs:
Bond order
not the way it is defined in QM!

## Slide 17
Reactive FFs
Why bond order?
Bond breaking is impossible!
Harmonic potential:
Physically correct limit: No interaction for infinitely separated atoms
Morse potential:
Bond breaking is possible!

## Slide 18
ReaxFF
van Duin, A. C. T.; Dasgupta, S.; Lorant, F.; Goddard, W. A. J. Phys. Chem. A 2001, 105, 9396–9409.

## Slide 19
Physisorption: All atoms, except S
Chemisorption: S atom
b=2.878 Å
Constructing your own FF: Example 1
The temperature when started rotating
didn’t depend too much on the alkyl size

## Slide 20
Akimov, A. V.; Williams, C.; Kolomeisky, A. B. J. Phys. Chem. C 2012, 116, 13816–13826.
Constructing your own FF: Example 2
Parameterization (PM6)
Validation
C60/Au diffusion coefficients

## Slide 21
Materials modeling FFs
Akimov, A. V.; Prezhdo, O. V. Chem. Rev. 2015, 115, 5797–5890.
Embedded atom method (EAM)
Systems with non-directional bonds (metals, alloys)
Modified EAM (MEAM)
Introduced bond directionality
(silicon, etc.)
MEAM92
Extended set of elements
(metals and non-metals)
Brenner, Tersoff-Brenner, REBO
Reactive potentials for hydrocarbons
ReaxFF
Charge-optimized many-body (COMBx)
Polarizable reactive potentials
Learn more:
Daw, M. S.; Baskes, M. I. Phys. Rev. Lett. 1983, 50, 1285−1288
Baskes, M. I. Phys. Rev. Lett. 1987, 59, 2666−2669
Baskes, M. I.; Nelson, J. S.; Wright, A. F. Phys. Rev. B 1989, 40, 6085−6100.
Baskes, M. I. Phys. Rev. B 1992, 46, 2727−2742.
Brenner, D. W. Phys. Rev. B 1990, 42, 9458−9471
Van Duin, A. C. T.; Dasgupta, S.; Lorant, F.; Goddard, W. A. J. Phys. Chem. A 2001, 105, 9396−9409
Yu, J.; Sinnott, S.; Phillpot, S. Phys. Rev. B 2007, 75, 085311

## Slide 22
Exercises: Running AA MD of H2O cluster
params["input_structure"] = "/23waters-aa.ent"
First, we cool the system down - optimization
T = 300 K
time = 5 ps
Tut2.1
T = 200 K
T = 100 K
Then, put some kinetic energy

## Slide 23
Exercises: Running RB MD of H2O cluster
params["input_structure"] = "/23waters.ent"
Now, do the same, but remove internal degrees of freedom
Tut2.1
Using rigid-body molecular
dynamics (RB-MD)
T = 100 K
T = 200 K
Internal degrees of freedom
act as “energy buffer”
The kinetics in AA and RB
bay be very different!

## Slide 24
Exercises: Running aa MD of SubPc/C60 cluster
Tut2.2
This is the same as before, but using a predefined library
Use: run_aa_md.py
High T – behaves wildly
Energy is well conserved
Optimized
10 ps of MD
Internal degrees of freedom
“absorb” energy leading
to low temperature
Assign T = 300 K after cooling

## Slide 25
Exercises: Running aa MD of SubPc/C60 cluster
Tut2.2
This is the same as before, but using another class
Use: run_aa_md_state.py
Gives the same as before (NVE ensemble)
ST.set_thermostat(therm)
"ensemble":"NVT"
10 ps of MD
One N center inversion occurs

## Slide 26
Tut2.3
Exercises: Computing specific heat capacity of gold
0.129
Reference value:

## Slide 27
m
m
Normal modes analysis

## Slide 28
m
m
M
are the displacements of all atoms in Cartesian coordinate system
Kinetic energy
Potential energy
Normal modes analysis

## Slide 29
Search the solutions
in the form:
Apply Lagrangian Equations of motion

## Slide 30
Apply Lagrangian Equations of motion
det = [
Non-trivial solution is when

## Slide 31
Normal modes
(translation)
Possible solutions

## Slide 32
Kinetic energy
Potential energy
In a general form